不饱和聚酯树脂、固化剂、偶联剂、钛白粉的检验

Unsaturated polyester resin, coupling agent, hardener

不饱和聚酯树脂（石英石专用树脂，以天和树脂DS-721-3为例）

Unsaturated polyester resin(used in quartz stone,to the TIAN HE resin(DS-721-3) in uviistone for example.)

| 天和树脂 TIAN HE RESIN |  |  |  |
| --- | --- | --- | --- |
| 液体树脂技术指标： Specifications for the liquid resin |  |  |  |
| 检验项目 Inspection item | DN-721-3 | 单位 Unit | 检测方法 Inspection standard |
| 外观 Appearance | 粘稠液体 Viscous liquid |  | 目视 Visual |
| 粘度 Viscosity | 0.6~0.9 | Pas(25℃) | GB7193.1 |
| 胶凝时间 Gelation time | 7~9 | min(25℃) | GB7193.6 |
| 酸值 Acidity | 22~25 | mgKOH/g | GB2895 |
| 固体含量 Solid percentage | ≥65~68 | % | GB7193.3 |
| 80 ℃稳定性 Stability in 80 ℃ | ≥ 24 | h | GB7193.5 |
| 色度（Pt-Co） Chroma | ≥25-35 | \ | GB7193.7 |
| 备注：凝胶时间为25℃空气浴50g树脂中加入0.5ml异辛酸钴溶液和0.5mlMEKP溶液。 Remark: Gelation time inspection way: under 25℃ air bath, mix 0.5ml different octylic acid cobalt solution and 0.5ml MEKP solution with 50g resin, and check it’s gelation time. |  |  |  |
| 固体树脂技术指标： Specifications for the solid resin |  |  |  |
| 外观 Appearance | 浇铸体无缺陷 Solid resin body no defect |  |  |
| 拉伸强度 Tensile strength | ≥70 | MPa | GB2568 |
| 拉伸弹性模量 Stretch elasticity modulus | ≥2900 | MPa | GB2568 |
| 断裂延伸率 Elongation at break | ≥5 | % | GB2568 |
| 弯曲强度 flexural strength | ≥100 | MPa | GB2570 |
| 弯曲弹性模量 Bend elasticity modulus | ≥3000 | MPa | GB2570 |
| 冲击强度 Impulse strength | ≥9 | KJ/m2 | GB2571 |
| 变形温度 Deformation temperature | ≥67 | ℃ | GB1634 |
| 巴氏硬度 - Barcol hardness | ≥38 | \ | GB3854 |
| 注：实验环境温度23±2℃ 相对湿度50±5% Remark: Testing temperature: 23±2℃, relative humidity: 50±5% |  |  |  |

验收标准：Acceptance standard

硅烷偶联剂KH560/570

Silane coupling agent KH560/570

验收标准：Acceptance standard

KH570:r-甲基丙烯酰氧(丙基三甲氧基硅烷)成分含量97%以上。

KH570: r-Methacryloyl oxygen(propyl trimethoxy silane) percentage composition: ≥97%

KH560:r-(2,3-环氧丙氧基)丙基三甲氧基硅烷成分含量97%以上。

KH560: r-2,3- epoxypropoxyl(propyl trimethoxy silane) percentage composition: ≥97%

中温固化剂（过氧化二乙基己酸叔丁酯）

Mesotherm hardener(Two ethyl tert butyl peroxide)

验收标准：Acceptance standard

外观：无色透明液体

Appearance: transparent liquid
过氧化物含量：＞97.0%（w/w）

Peroxide content percentage: ＞97.0%（w/w）
活性氧：＞7.18%

Reactive oxygen：＞7.18%

三：色料 Pigment

在人造石英石原料选择过程中，为了保证材料的耐候性，尽量选用无机色料。但耐候性稳定的碳黑，大红等有机原料也可使用。石英石中常用色料有：

德国拜耳色粉（4920黄、4130红、4330黑）、酞青兰粉、酞青绿粉、大红粉、U-黑粉、R-902+钛白粉。

In order to guarantee the weather resistance of the raw material, normally we use inorganic pigment as artificial quartz stone raw material. But some organic materials like carbon black, bright red which with stable weather resistance also can be used.

Normally we use the pigment as below:

4920 yellow, 4130 red, 4330 black, phthalocyanine blue, phthalocyanine green, bright red, U-black, R-902+Tio2.