石英石原材料及检测标准

Inspection standard for A.Q.STONE raw material

一、颗粒及粉料 grains and powder

透玻5-6、6-8、8-16、16-30、30-50目.

Crystal glass mesh: 5#-6#、6#-8#、8#-16#、16#-30#、30#-50#

镜玻6-8、8-16、16-30、30-50目.

Mirror glass mesh: 6#-8#、8#-16#、16#-30#、30#-50#

石英砂4-6、6-8、8-10、10-20、20-40、40-70、70-140目.

Quartz sand mesh: 4#-6#、6#-8#、8#-10#、10#-20#、20#-40#、40#-70#、70#-140#

石英粉250目、325目、400目。

Quartz powder mesh: 250#, 325#, 400#

按照不同产地、不同规格标识清楚，整齐堆放。

Lay in position according to different supplier, different specification

验收标准：Acceptance standard

| 项目Item |  | 合格Qualified | 不合格Disqualification |
| --- | --- | --- | --- |
| 普通的 石英砂 透玻 Quartz sand, crystal glass | 大颗粒 Larger size | 不可有 Without larger size | 有 With larger size |
|  | 杂色 motley | 100克里只有5颗或以下不明显杂色，且杂色颗粒粒径小于等于该目数里最大颗粒粒径的50% 1, ≦5pcs unconspicuous motley within 100g 2, Motley grain size must less than or equal to 50% of the biggest grain size of the checking batch | 100克里有5颗以上明显杂色，且杂色颗粒粒径大于该目数里最小颗粒粒径的50%（特殊要求除外） 1, ＞5pcs unconspicuous motley within 100g - 2, Motley grain size must larger than 50% of the most small grain size of the checking batch (except special requirements) |
|  | 杂物 impurity | 100克里有2颗或以下不明显杂物，且颗粒小于等于该目数里的最大颗粒80% 1, ≦2pcs unconspicuous impurity within 100g 2, Impurity grain size must less than or equal to 80% of the biggest grain size of the checking batch | 100克里有2颗或以上明显杂物，且颗粒大于该目数里最小颗粒的20 1, ＞2pcs unconspicuous impurity within 100g - 2, Impurity grain size must larger than 20% of the most small grain size of the checking batch |
|  | 颜色 color | 透明或白色。同一批相同。 Transparent or white, same color in same batch | 同一批颜色混乱 Different color in same batch |
|  | 水份 moisture | 0.5%或以下 ≦0.5% | 超过0.5%以上 ﹥0.5% |
| 镜玻 Mirror glass | 大颗粒 Larger size | 不可有 Without larger size | 有 With larger size |
|  | 杂色 motley | 100克里只有5颗或以下不明显杂色，且杂色颗粒粒径小于等于该目数里最大颗粒粒径的50% 1, ≦5pcs unconspicuous motley within 100g 2, Motley grain size must less than or equal to 50% of the biggest grain size of the checking batch | 100克里有5颗以上明显杂色，且杂色颗粒粒径大于该目数里最小颗粒粒径的50%（特殊要求除外） 1, ＞5pcs unconspicuous motley within 100g - 2, Motley grain size must larger than 50% of the most small grain size of the checking batch (except special requirements) |
|  | 杂物 impurity | 100克里有2颗或以下不明显杂物，且杂物颗粒粒径小于等于该目数里的最大颗粒粒径的80% 1, ≦2pcs unconspicuous impurity within 100g 2, Impurity grain size must less than or equal to 80% of the biggest grain size of the checking batch | 100克里有2颗或以上明显杂物，且杂物颗粒粒径大于该目数里最小颗粒粒径的20 % 1, ＞2pcs unconspicuous impurity within 100g 2, Impurity grain size must larger than 20% of the most small grain size of the checking batch |
|  | 脱色 fade | 不可有 No fade | 有 With fade |
| 石英粉 Quartz powder | 颜色 color | 和试样相同 Nearly or Same as sample | 颜色与试样相差太大 Much different from sample |
|  | 筛余 residue on sieve | 10 %或以下 ≦10% | 超过10 %以上 ﹥10% |
|  | 水份 moisture | 0.5%或以下 ≦0.5% | 超过0.5%以上 ﹥0.5% |

注：Remarks

（1）大颗粒：超过该目数里最大颗粒。

Larger size: larger than the ordered grain.

（2）杂色：黑点、白点、黄点等，有色颗粒。

Motley: black spot, white spot, yellow spot, colored grain

（3）杂物：玻璃胶、木屑、包装带、石头等，非玻璃、石英物质。

Impurity: glass cement, sawdust, package tape, stone ect.

(4) 颗粒大于20#以上的透玻、镜玻，在破碎前玻璃片和镜片的厚度要≥4mm。

If the crystal glass and mirror glass grains bigger then 20#, the pieces of crystal glass and mirror glass before crushed thickness must more the 4mm.

| 石英砂目数与粒径大小对照表 Grain size |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| A.S.T.M(mesh) | MM | A.S.T.M(mesh) | MM | A.S.T.M(mesh) | MM |
| 6# | 3.350 | 20# | 0.850 | 120# | 0.125 |
| 70# | 2.800 | 25# | 0.710 | 140# | 0.106 |
| 10# | 2.000 | 40# | 0.425 | 200# | 0.075 |
| 12# | 1.700 | 60# | 0.250 | 230# | 0.063 |
| 14# | 1.400 | 80# | 0.180 | 325# | 0.045 |
| 18# | 1.000 | 100# | 0.150 | / |  |